## Elmer Wallace Ltd

30 Nasmyth Road South, Colquhoun Park, Hillington Ind Estate Glasgow G52 4RE

Tel: 0141 810 5530                                                                      Fax: 0141 810 5539

## ALUMINIUM CLEANER 101

# Operating Instructions

## General

Aluminium Cleaner 101 is a mildly acidic solution used for cleaning and pickling of aluminium. It acts by removing the oxide layer, while cleaning and degreasing the surface. It can be applied before welding or used afterwards to remove welding burn. It is also used before painting to give a clean surface for improved adherence.

## Application

Aluminium Cleaner 101 is sprayed evenly across the surface using the hand sprayer or brushed onto the area to be cleaned. Allow the solution 1 – 2 min to work then rinse thoroughly with water.

If used to remove the oxide layer prior to welding, paint or spray onto the weld area then wipe off excess after 1 – 2 mins and ensure surface is dry.

This product can also be used for light cleaning of stainless steel surfaces.

## Yield

1 kg of Aluminium Cleaner 101 is sufficient for approx 20m2 of surface area.

## Health and Safety

Please note the hazard warnings on the product label and the separate safety data sheet.

## Environmental Protection

Used Aluminium Cleaner 101 solutions must not be disposed of in drains without treatment.

## Disclaimer

This issue replaces all previous issues.  The information is provided to the best of our knowledge and conscience and conforms to the laboratory and field experience at the time of going to press. However, it must only be regarded as non-binding guidelines which have to be adapted to requirements.  Since the use of our products lies beyond our control, we can only accept liability for the perfect standard quality at the time of delivery.  Consequential losses will only be recognised if this was expressly agreed before use in writing, stating the warranted characteristics.