METAL SPRAY POWDERS

Machinability -1-3 grind only 3-7 tipped tools 7+ hand tools

| ALLOY/ NAME | NOMINAL COMPOSITION |
| --- | --- |

HARDNESS

RC

SERVICE CONDITIONS RESISTANCE TO:

Abrasion Corrosion Impact Heat Galling Machine

MELTING POINT

0C

MACHINA

| ABILITY | TYPICAL APPLICATIONS |
| --- | --- |
| EWP-weld 16N |

1.8 Silicon

1.2 Boron

22.0 Copper

| Bal Nickel | 14-16 |
| --- | --- |
| 7.5 | Formulated for the repair of defects in iron castings. Excellent weld characteristics and colour match. |

EWP-weld 20N

0.1 Carbon

1.0 Chromium

2.4 Silicon

1.3 Boron

1.0 Iron

| Bal Nickel | 18-20 | F | EX | EX | VG | G | VG | 1060 | 6.5 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

Specially designed for repair to glass moulds and cast iron, but can be used equally well on mild steel and stainless steel. Deposits can be finished with a file.

General purpose machinable repair.

EWP-weld 30N

0.25 Carbon

5.0 Chromium

2.4 Silicon

1.7 Boron

2.0 Iron

| Bal Nickel | 28-30 |
| --- | --- |
| 5.5 |

A nickel-based alloy for repairs to cast iron, for general wear resistance and hard facing applications.

Resistant to elevated temperatures and corrosion.

EWP-weld 40N

0.4 Carbon

9.0 Chromium

2.4 Silicon

1.8 Boron

2.5 Iron

| Bal Nickel | 38-40 | VG | EX | EX | VG | VG | VG | 1100 | 4.5 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

Moulds and Plungers in Glass Industry. Dies bearing surfaces, metering pins, gear teeth. Valves and valve seats in Chemical Industry.

Excellent hard facing properties.

EWP-weld 50N

0.5 Carbon

12.0 Chromium

3.0 Silicon

2.5 Boron

3.5 Iron

| Bal Nickel | 48-50 | VG | EX | VG | EX | VG | G | 1070 | 2.5 | Extrusion Screws, Pump sleeves and shafts, tyre moulds. Diesel engine valves, press tools jigs and dies, entry and twisting rollers in steel mills. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| EWP-weld 60N |

0.7 Carbon

15.0 Chromium

4.5 Silicon

3.25 Boron

4.5 Iron

| Bal Nickel | 58-60 | EX | EX | G | VG | EX | GRIND ONLY | 1040 | 1.5 | Where extreme resistance to abrasion and corrosion is required. For use on shafts, gears, bushings, cams, thrust collars, pump seal rings, rocker arms etc. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |