# 76E Stainless Steel 3-in-1

Light Pickle, Cleaner & Passivator

The 76E stainless steel pickling cleaner is used to remove Iron (rust) contamination, light annealing colours, oil and grease. It also brightens and passivates the metal surfaces in a single operation. This solution meets the requirements detailed in ASTM A380-13 & A967-13. The solution can be applied by acid resistant brushes, immersion in a bath or by using a chemical resistant spray unit such as the Antox hand operated sprayer. <0}

## {0>Anwendung und Ablauf<}97{>Application and Procedure<0}

Before commencing work all safety precautions must be observed and the correct protective equipment used (see MSDS).

The 76E cleaner is ready to use and is applied to a dry metal surface. {0>Die Wirkung von Antox 75 E Extra kann durch die Verwendung eines Schleifvlieses unterstützt werden.<}0{>When removing Iron contamination a minimum contact time of 20 minutes is required for the chemical reaction to take place. The ideal operating temperature for best results is around 18 - 22° C. Work routines should be avoided in direct sunlight (due to hazard of premature drying). The effect of 76E cleaner can be supported by the use of a soft abrasive fabric.<0}{0>Die optimale Einwirkzeit ist in einem Vorversuch zu ermitteln.<}0{> <0}

<0}Neutralise with 10% solution of the alkaline based Mainclean brushed onto the surface, sprayed or dosed through Jet wash then rinse with cold water. This works in three ways, it neutralizes the acid in-situ so that it does not contaminated other areas, stops the formation of the “spilt milk” effect associated with Phosphoric acid and finally ensures that the solution washed off is about ph 7. Although the acids are neutralised local waste water regulations must be observed.

## {0>Einwirkzeit<}97{>Reaction Time Periods<0}

{0>Reinigung rost- und säurebeständiger Stahl, Edelstahl<}82{>Rust and acid-resistant steels, stainless steels	<0}	20{0>15 - 30 Minuten<}97{> -30 minutes<0}

{0>Entfernen von Anlauffarben auf III d-Blechen<}0{>Removal of annealing colours on III d sheets<0}		{0>30 - 60 Minuten<}100{>30 -60 minutes<0}

{0>Mit 1 kg Antox 75 E Extra können ca. 20 m2 Fläche behandelt werden.<}0{>1 litre of 76E cleaner is sufficient for approx. 20 m2 of surface area.<0}

## {0>Allgemeiner Hinweis<}0{>General Remarks<0}

This 76E cleaner contains no hydrochloric acid or chlorides.<0}

## {0>Gefahrenhinweise und Sicherheitsratschläge<}97{>Notes on hazards and suggestions for safety precautions<0}

This 76E cleaner contains phosphoric, nitric and hydrofluoric acid. It is classified as extremely toxic if swallowed.<0} Avoid c{0>Berührung mit der Haut verursacht Verätzungen.<}82{>ontact with the skin as it causes acid burns. <0}{0>An einem gut gelüfteten Ort verarbeiten und aufbewahren (Behälter dicht verschliessen).<}97{>Process and store in a well-ventilated place (the cans should be tightly closed).<0} {0>Bei unzureichender Lüftung Atemschutzgerät tragen.<}97{>Breathing apparatus should be used when ventilation facilities are insufficient.<0} {0>Bei der Arbeit geeignete Schutzbrille, Schutzhandschuhe und Schutzkleidung tragen.<}97{>Appropriate protective goggles, gloves and clothing should be worn whilst working.

<0}

{0>Bei Berührung mit den Augen gründlich mit Wasser abspülen und den Arzt konsultieren.<}97{>Contact with the eyes should be treated by thorough rinsing with water and thereafter a doctor should be consulted.<0} {0>Beschmutzte, getränkte Kleidung sofort ausziehen.<}97{>Contaminated and soaked protective clothing should be immediately changed.<0} {0>Bei Unwohlsein sofort Arzt zuziehen (unbedingt Sicherheitsdatenblatt, Merkblatt- und/oder Etikette vorzeigen).<}97{>A doctor should be consulted if nausea is experienced (the doctor should be shown the notes on safety precautions, the product notes or the product label).<0}

{0>Darf nicht in die Hände von Kindern gelangen.<}97{>These products should not be accessible to children.<0} {0>Nur zur gewerblichen Nutzung.<}100{>For commercial and industrial use only.<0}

## {0>Entsorgung<}97{>Disposal<0}

{0>Antox 75 E Extra sowie dessen Spülwässer dürfen nicht unbehandelt in die Kanalisation gelangen.<}89{>Neither 76E cleaner nor the rinsing water may be disposed of in the public sewers in an untreated state.<0} {0>Die Abwässer sind sauer und enthalten Metalloxyde des behandelten Materials.<}88{>The waste water is acidic and contains metal oxides from the treated metal.<0} {0>Aufbereitung über eine geeignete Neutralisationsanlage oder Entsorgung durch ein zugelassenes Unternehmen.<}97{>Appropriate treatment should be carried out in a suitable neutralisation plant or disposal undertaken via a licensed waste disposal enterprise.<0} {0>Die örtlichen Abwasser-Vorschriften sind zu beachten.<}97{>The local waste water regulations are to be observed.<0}

## Disclaimer

This issue replaces all previous issues.  The information is provided to the best of our knowledge and conscience and conforms to the laboratory and field experience at the time of going to press. However, it must only be regarded as non-binding guidelines which have to be adapted to requirements.  Since the use of our products lies beyond our control, we can only accept liability for the perfect standard quality at the time of delivery.  Consequential losses will only be recognised if this was expressly agreed before use in writing, stating the warranted characteristics.