| PRODUCT & PACK SIZE | DESCRIPTION | APPLICATION | REACTION TIME (18 - 22ºC) | USAGE | COMMENTS |
| --- | --- | --- | --- | --- | --- |
| ANTOX 71E PLUS Pickling paste 2kg & 10kg | Clear thick paste | Stir well before use. Apply with acid resistant brush. Neutralise with Antox NP & Jet wash with cold water. | Stainless Steel 15 - 60 mins Nickel & Nickel alloys 5 - 20 mins Copper-Nickel alloys 5 - 20 mins Titanium & alloys - by trials | 1 kg will treat 50 - 80 m length of weld burn. | Thixotropic properties enable vertical surfaces to be coated. Leaves white “halo” on area pickled |
| ANTOX 3D Pickling paste 2kg | Clear thick non-toxic pickling paste. For bright polished surfaces. Can also used for Aluminium | Stir well before use. Apply with acid resistant brush. Neutralise with Antox NP & Jet wash with cold water | Stainless Steel 30 - 60 mins Nickel & Nickel alloys 5 - 20 mins Copper-Nickel alloys 5 - 20 mins Aluminium & alloys 5 - 20 mins | 1 kg will treat 80 - 120 m length of weld burn. | Does not leave “halo” around area pickled. Used for lighter TIG/MIG weld burn. |
| ANTOX - NP Neutralising paste 2kg | Thick white paste | Stir well before use. Apply with the same brush on top of pickling paste. Jet wash with cold water. | Dependent on amount of pickling paste to be neutralised. Reaction is complete when foaming & bubbling has stopped. | 1 kg will treat 50 - 80 m length of weld which has been pickled. | Although the acids are neutralised local waste water regulations must be observed. |
| ANTOX 73E SG Spray pickle 10kg | Thick creamy liquid. Use colour indicator for economy. Pickle seams & surfaces in one operation. | Mix well to obtain an even consistency similar to wallpaper paste. Apply with acid resistant spray unit. Neutralise with 5% solution of Mainclean dosed through Jet wash then rinse with cold water. | Stainless Steel 15 - 60 mins Nickel & Nickel alloys 5 - 20 mins Copper-Nickel alloys 5 - 20 mins | 1 kg will treat 4 - 6 sq.metres of surface area. | Thixotropic properties enable vertical surfaces to be coated. Colour indicator makes spray visible & reduces Nitric odours. Surface requires passivation treatment after spray pickling. |
| ANTOX 80E Bath pickle 25kg | Clear liquid | Acid resistant plastic bath diluted 1:1 to 1:3 Add acid to water | Stainless Steel 15 - 60 mins | 1 kg will treat 4 sq. metres of surface area. | Reaction times are dependent on the condition of the bath, air temperature & surface condition. Surface requires passivation treatment after bath pickling. |
| PRODUCT & PACK SIZE | DESCRIPTION | APPLICATION | REACTION TIME (18 - 22ºC) | USAGE | COMMENTS |
| 90E Passivator 5kg | Clear liquid used to form the protective passivation layer after pickling. | Apply by acid resistant brush, spray or bath. Neutralise with 5% solution of Mainclean dosed through Jet wash then rinse with cold water. | Stainless Steels 20- 30 mins | 1 kg will treat 20 - 25 sq. metres of surface area. | Accelerates the formation of the Chromium Oxide passive layer. Use after pickling or mechanical surface finishing. |
| 76E Passivator & Pickling cleaner 10kg | Non-toxic acid solution which passivates, removes Iron contamination, cleans & brightens in one operation. | Apply by acid resistant brush, spray or bath. Neutralise with 5% solution of Mainclean dosed through Jet wash then rinse with cold water. | Stainless Steel 20 - 30 mins Nickel & Nickel alloys 5 - 20 mins | 1 kg will treat 20 - 25 sq. m. surface area | Removes light annealing marks, rust staining, oil, grease and other contamination while forming the Chromium Oxide protective layer. |
| 75E Rust Remover 95E Rust Remover & Passivator 5kg | Non-toxic mild acid solution used to clean & brighten surfaces. | Apply by acid resistant brush, spray or bath. Neutralise with 10% solution of Mainclean dosed through Jet wash then rinse with cold water. | Stainless Steel 20 - 30 mins Nickel & Nickel alloys 5 - 20 mins | 1 kg will treat 20 - 25 sq. m. surface area | Removes rust marks, oil, grease and other contamination. Antox 95E also restores the passive layer in the same operation |
| EWP 51 Citric Passivator & Cleaner 25kg | Steel Stainless Steel Aluminium Glass-lined vessels | As a controlled foaming material, EWP 51 is highly effective for both circulation-in-place and manual cleaning at about 10% dilution. | Removes milk, beer & urine stain, lime scale and other mineral deposits as well as food residue from equipment in dairies, breweries, pharmaceutical plants, food processing and animal research centres. | EWP 51 Citric acid solution passivates Stainless steel according to ASTM A380-06 & ASTM A967. | It is used as a mild passivating solution where the more “acidic” Nitric acid solutions are not suitable, particularly in food & and pharmaceutical applications. |
| ANTOX 2001T 400g & 1kg | Grey paste for cleaning & polishing. | Brush, cloth or sponge. Wash off with water. | Stainless Steel 5 - 20 mins | Apply a thin even coat to surfaces. | Polishes surfaces & removes contamination without dulling. |