| ALLOY IDENTIFICATION P.M.I. Positive Material Identification ASTM DESIGNATION E 1476 CHEMICAL SPOT CHECKS Simple test for identification of 316 alloy |  |
| --- | --- |
| Code 23.100 CELMO Reagent Molybdenum for AISI 304 vs 316 To distinguish between AISI 316 and 304 you only need one reagent and one step |  |
| Apply a drop of solution to the (abraded) metal surface. Leave for 1 – 5 minutes. If it turns brown it is 316, no change then it is not 316. Kit for approx. 550 tests (long shelf life) |  |