#### METAL SPRAY POWDERS

Machinability -1-3 grind only 3-7 tipped tools 7+ hand tools

| ALLOY/ NAME | NOMINAL COMPOSITION | ### HARDNESS RC | SERVICE CONDITIONS RESISTANCE TO: # Abrasion Corrosion Impact Heat Galling Machine |  |  |  |  |  | MELTING POINT 0C | MACHINA ABILITY | ## TYPICAL APPLICATIONS |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| EWP-weld 16N | 1.8 Silicon 1.2 Boron 22.0 Copper Bal Nickel | 14-16 |  |  |  |  |  |  |  | 7.5 | Formulated for the repair of defects in iron castings. Excellent weld characteristics and colour match. |
| EWP-weld 20N | 0.1 Carbon 1.0 Chromium 2.4 Silicon 1.3 Boron 1.0 Iron Bal Nickel | 18-20 | F | EX | EX | VG | G | VG | 1060 | 6.5 | Specially designed for repair to glass moulds and cast iron, but can be used equally well on mild steel and stainless steel. Deposits can be finished with a file. General purpose machinable repair. |
| EWP-weld 30N | 0.25 Carbon 5.0 Chromium 2.4 Silicon 1.7 Boron 2.0 Iron Bal Nickel | 28-30 |  |  |  |  |  |  |  | 5.5 | A nickel-based alloy for repairs to cast iron, for general wear resistance and hard facing applications. Resistant to elevated temperatures and corrosion. |
| EWP-weld 40N | 0.4 Carbon 9.0 Chromium 2.4 Silicon 1.8 Boron 2.5 Iron Bal Nickel | 38-40 | VG | EX | EX | VG | VG | VG | 1100 | 4.5 | Moulds and Plungers in Glass Industry. Dies bearing surfaces, metering pins, gear teeth. Valves and valve seats in Chemical Industry. Excellent hard facing properties. |
| EWP-weld 50N | 0.5 Carbon 12.0 Chromium 3.0 Silicon 2.5 Boron 3.5 Iron Bal Nickel | 48-50 | VG | EX | VG | EX | VG | G | 1070 | 2.5 | Extrusion Screws, Pump sleeves and shafts, tyre moulds. Diesel engine valves, press tools jigs and dies, entry and twisting rollers in steel mills. |
| EWP-weld 60N | 0.7 Carbon 15.0 Chromium 4.5 Silicon 3.25 Boron 4.5 Iron Bal Nickel | 58-60 | EX | EX | G | VG | EX | GRIND ONLY | 1040 | 1.5 | Where extreme resistance to abrasion and corrosion is required. For use on shafts, gears, bushings, cams, thrust collars, pump seal rings, rocker arms etc. |